## Slide 1: Review: Steps in a Heterogeneous Catalytic Reaction
1. Mass transfer of A to surface
2. Diffusion of A from pore mouth to internal catalytic surface
3. Adsorption of A onto catalytic surface
4. Reaction on surface
5. Desorption of product B from surface
6. Diffusion of B from pellet interior to pore mouth
7. Diffusion of B from external surface to the bulk fluid (external diffusion)
Ch 10 assumes steps 1,2,6 & 7 are fast, so only steps 3, 4, and 5 need to be considered

## Slide 2: Review: Guidelines for Deducing Mechanisms
More than 70% of heterogeneous reaction mechanisms are surface reaction limited
  When you need to propose a rate limiting step, start with a surface reaction limited mechanism unless you are told otherwise
If a species appears in the numerator of the rate law, it is probably a reactant
If a species appears in the denominator of the rate law, it is probably adsorbed in the surface

## Slide 3: L19: External Diffusion Effects
Up until now we have assumed adsorption, surface reaction, or desorption was rate limiting, which means there are no diffusion limitations
In actuality, for many industrial reactions, the overall reaction rate is limited by the rate of mass transfer of products and reactants between the bulk fluid and the catalyst surface
  External diffusion (today)
  Internal diffusion (L20, L21 & L21b)
  Goal: Overall rate law for heterogeneous catalyst with external diffusion limitations. This new overall reaction rate would be inserted into the design equation to get W, XA, CA, etc
External diffusion
Internal diffusion

## Slide 4: Mass Transfer
Diffusion: spontaneous intermingling or mixing of atoms or molecules by random thermal motion
External diffusion: diffusion of the reactants or products between bulk fluid and external surface of the catalyst
Molar flux (W)
  Molecules of a given species within a single phase will always diffuse from regions of higher concentrations to regions of lower concentrations
  This gradient results in a molar flux of the species, (e.g., A), WA (moles/area•time), in the direction of the concentration gradient
  A vector:

## Slide 5: Molar Flux W & Bulk Motion BA
Molar flux consists of two parts
  Bulk motion of the fluid, BA
  Molecular diffusion flux relative to the bulk motion of the fluid produced by a concentration gradient, JA
  WA = BA + JA (total flux = bulk motion + diffusion)
Bulk flow term for species A, BA: total flux of all molecules relative to fixed coordinates (SWi) times the mole fraction of A (yA):
Or, expressed in terms of concentration of A & the molar average velocity V:
The total molar flux of A in a binary system composed of A & B is then:
←In terms of concentration of A
←In terms of mol fraction A

## Slide 6: Diffusional Flux of A, JA & Molar Flux W
Diffusional flux of A resulting from a concentration difference, JA, is related to the concentration gradient by Fick’s first law:
c: total concentration DAB: diffusivity of A in B yA: mole fraction of A
Putting it all together:
molar flux of A in binary system of A & B
General equation
Effective diffusivity, DAe: diffusivity of A though multiple species
  WA = JA + BA (total flux = diffusion + bulk motion)

## Slide 7: Simplifications for Molar Flux
Molar flux of A in binary system of A & B
General equation:
For constant total concentration: cDAByA = DABCA
When there is no bulk flow:
For dilute concentrations, yA is so small that:
For example, consider 1M of a solute diffusing in water, where the concentration of water is 55.6 mol water/dm3
  WA = JA + BA (total flux = diffusion + bulk motion)

## Slide 8: Evaluation of Molar Flux
  Type 1: Equimolar counter diffusion (EMCD)
  For every mole of A that diffuses in a given direction, one mole of B diffuses in the opposite direction
  Fluxes of A and B are equal in magnitude & flow counter to each other: WA = - WB
0 bulk motion ≈ 0
  Type 2: Dilute concentration of A:
0
  Type 3: Diffusion of A though stagnant B: WB=0
0
  Type 4: Forced convection drives the flux of A. Diffusion in the direction of flow (JA) is tiny compared to the bulk flow of A in that direction (z):
0 diffusion ≈ 0
volumetric flow rate
cross-sectional area

## Slide 9: Boundary Conditions
Boundary layer
  Hydrodynamics boundary layer thickness: distance from a solid object to where the fluid velocity is 99% of the bulk velocity U0
  Mass transfer layer thickness: distance  from a solid object to where the concentration of the diffusing species is 99% of the bulk concentration
Typically diffusive transport is modelled by treating the fluid layer next to a solid boundary as a stagnant film of thickness 

CAb
CAs
In order to solve a design equation that accounts for external diffusion limitations we need to set the boundary conditions
CAs: Concentration of A at surface CAb: Concentration of A in bulk

## Slide 10: Types of Boundary Conditions
Concentration at the boundary (i.e., catalyst particle surface) is specified:
  If a specific reactant concentration is maintained or measured at the surface, use the specified concentration
  When an instantaneous reaction occurs at the boundary, then CAs≈0
Flux at the boundary (i.e., catalyst particle surface) is specified:
  No mass transfer at surface (nonreacting surface)
  Reaction that occurs at the surface is at steady state: set the molar flux on the surface equal to the rate of reaction at the surface
  Convective transport across the boundary layer occurs
reaction rate per unit surface area (mol/m2·sec)
Planes of symmetry: concentration profile is symmetric about a plane
  Concentration gradient is zero at the plane of symmetry
Radial diffusion in a tube:
r
r
Radial diffusion in a sphere

## Slide 11: Correlation for Convective Transport Across the Boundary Layer
  For convective transport across the boundary layer, the boundary condition is:
The mass transfer coefficient for a single spherical particle is calculated from the Frössling correlation:
kc: mass transfer coefficient DAB: diffusivity (m2/s)
dp: diameter of pellet (m) Sh: Sherwood number (dimensionless)
n: kinematic viscosity or momentum diffusivity (m2/s); n=m/r
r: fluid density (kg/m3) m: viscosity (kg/m·s)
U: free-stream velocity (m/s) dp: diameter of pellet (m)
DAB: diffusivity (m2/s)

## Slide 12: Rapid Rxn on Catalyst Surface
Spherical catalyst particle in PBR
Liquid velocity past particle U = 0.1 m/s
Catalyst diameter dp= 1 cm = 0.01 m
Instantaneous rxn at catalyst surface CAs≈0
Bulk concentration CAb= 1 mol/L
n ≡ kinematic viscosity = 0.5 x 10-6 m2/s
DAB = 1x10-10 m2/s
Determine the flux of A to the catalyst particle
CAs=0
0.01m
CAb= 1 mol/L
The velocity is non-zero, so we primarily have convective mass transfer to the catalyst particle:
Compute kC from Frössling correlation:

## Slide 13: Rapid Rxn on Catalyst Surface
Spherical catalyst particle in PBR
Liquid velocity past particle U = 0.1 m/s
Catalyst diameter dp= 1cm = 0.01m
Instantaneous rxn at catalyst surface CAs≈0
Bulk concentration CAb= 1 mol/L
n ≡ kinematic viscosity = 0.5 x 10-6 m2/s
DAB = 1x10-10 m2/s
Determine the flux of A to the catalyst particle
CAs=0
0.01m
CAb= 1 mol/L
The velocity is non-zero, so we primarily have convective mass transfer to the catalyst particle:
Computed kC from Frössling correlation:
Because the reactant is consumed as soon as it reaches the surface

## Slide 14
For the previous example, derive an equation for the flux if the reaction were not instantaneous, and was instead at steady state (WA|surface =-rA”) and followed the kinetics: -rAS’’=krCAs (Observed rate is not diffusion limited)
Because the reaction at the surface is at the steady state & not instantaneous:
So if CAs were in terms of measurable species, we would know WA,boundary
Use the equality to put CAs in terms of measurable species (solve for CAs)
Plug into -r’’As
Rapid rxn, kr>>kc→ kc in denominator is negligible
Diffusion limited
Slow rxn, kr<<kc→ kr in denominator is negligible
Reaction limited

## Slide 15: Mass Transfer & Rxn Limited Reactions
transport limited regime
-rA’
(U/dp)1/2
(fluid velocity/particle diameter)1/2
reaction limited regime
When measuring rates in the lab, use high velocities or small particles to ensure the reaction is not mass transfer limited

## Slide 16: Mass Transfer & Rxn Limited Reactions
transport limited regime
-rA’
(U/dp)1/2 = (fluid velocity/particle diameter)1/2
reaction limited regime
Proportionality is useful for assessing parameter sensitivity

## Slide 17: Mass Transfer Limited Rxn in PBR
ac: external surface area of catalyst per volume of catalytic bed (m2/m3)
f: porosity of bed, void fraction dp: particle diameter (m)
r’’A: rate of generation of A per unit catalytic surface area (mol/s·m2)
A steady state mole balance on reactant A between z and z + z :
Divide out AcDz:
Take limit as Dz→0:
Put Faz and –rA’’ in terms of CA:
Axial diffusion is negligible compared to bulk flow (convection)
Substitute into the mass balance
0

## Slide 18: Mass Transfer Limited Rxn in PBR
At steady-state:
Molar flux of A to particle surface = rate of disappearance of A on the surface
mass transfer coefficient kc =DAB/d (s-1) d: boundary layer thickness
CAs: concentration of A at surface CA: concentration of A in bulk
Substitute
CAs ≈ 0 in most mass transfer-limited rxns
Rearrange & integrate to find how CA and the r’’A varies with distance down reactor

## Slide 19: Review: Heterogeneous Catalyst
We have looked at cases where
  Adsorption, surface reaction, or desorption is rate limiting
  External diffusion is rate limiting
  Internal diffusion is rate limiting- today
Next time: Derive an overall rate law for heterogeneous catalyst where the rate limiting step as any of the 7 reaction steps. This new overall reaction rate would be inserted into the design equation to get W, XA, CA, etc

## Slide 20: Review: Types of Boundary Conditions
Concentration at the boundary (i.e., catalyst particle surface) is specified:
  If a specific reactant concentration is maintained or measured at the surface, use the specified concentration
  When an instantaneous reaction occurs at the boundary, then CAs≈0
Flux at the boundary (i.e., catalyst particle surface) is specified:
  No mass transfer at surface (nonreacting surface)
  Reaction that occurs at the surface is at steady state: set the molar flux on the surface equal to the rate of reaction at the surface
  Convective transport across the boundary layer occurs
reaction rate per unit surface area (mol/m2·sec)
Planes of symmetry: concentration profile is symmetric about a plane
  Concentration gradient is zero at the plane of symmetry
Radial diffusion in a tube:
r
r
Radial diffusion in a sphere

## Slide 21: Review: Transport & Rxn Limited Rates
  transport limited regime
  (Convective transport across boundary layer)
-rA’
(U/dp)1/2
(fluid velocity/particle diameter)1/2
reaction limited regime:
When measuring rates in the lab, use high velocities or small particles to ensure the reaction is not mass transfer limited
Used kc(CAb-CAs)=krCAS to solve for CAs & plugged back into –r”As= krCAS

## Slide 22: Review: Mass Transfer Limited Rxn in PBR
ac: external surface area of catalyst per volume of catalytic bed (m2/m3)
f: porosity of bed, void fraction dp: particle diameter (m)
r’’A: rate of generation of A per unit catalytic surface area (mol/s·m2)
Ac: cross-sectional area of tube containing catalyst (m2)
A steady state mole balance on reactant A between z and z + z :
Divide out AcDz and take limit as Dz→0
Put Faz and –rA’’ in terms of CA
Assume that axial diffusion is negligible compared to bulk flow
Assume molar flux of A to surface = rate of consumption of A at surface
Rearrange, integrate, and solve for CA and r’’A

## Slide 23: Shrinking Core Model
Solid particles are being consumed either by dissolution or reaction
  The amount of the material being consumed is shrinking
  Drug delivery (pill in stomach)
  Catalyst regeneration
Regeneration of catalyst by burning off carbon coke in the presence of O2
Begins at the surface and proceeds to the core
Because the amount of carbon that is consumed (burnt off) is proportional to the surface area, and the amount of carbon that is consumed decreases with time

## Slide 24: Catalyst Regeneration
Coking-deactivated catalyst particles are reactivated by burning off the carbon
R0
R
r
r+r
O2
CO2
Oxygen (A) diffuses from particle surface (r = R0, CA = CA0) through the porous pellet matrix to the unreacted core (r = R, CA = 0)
Reaction of O2 with carbon at the surface of the unreacted core is very fast
CO2 generated at surface of core diffuses out
Rate of oxygen diffusion from the surface of the pellet to the core controls rate of carbon removal
Though the core of carbon (from r = 0 to r = R0) is shrinking with time (unsteady state), we will assume the concentration profile at any time is the steady state profile over distance (R0- R): quasi-steady state assumption (QSSA)
r : radius R0:outer radius of particle R: radius of unreacted core r = 0 at core
What is the rate of time required for the core to shrink to a radius R?

## Slide 25: Mole Balance on O2 From r to r+Dr
Rate in - rate out + gen = accum
R0
R
r
r+r
O2
CO2
Oxygen reacts at the surface, not in this region
Divide by -4pDr:
Take limit as Dr→0:
Put WAr in terms of conc of oxygen (CA)
For every mole of O2 that enters, a mol of CO2 leaves → WO2=-WCO2
De: effective diffusivity
Plug WAr into mole balance:
Divide out –De:

## Slide 26: Mole Balance on O2 From r to r+Dr (2)
R0
R
r
r+r
O2
CO2
Use boundary conditions to determine the concentration profile (CA/CA0) in terms of the various radii (R, R0 & r)
At r = R0, CA= CA0 and at r = R, CA= 0
First use CA=0 when r = R to determine K2
For any r:
Next solve for when r = R0 & CA=CA0
Take the ratio to determine CA/CA0

## Slide 27: Oxygen Concentration Profile & Flux
Chart: r
| 5.0 | 6.0 | 7.0 | 8.0 | 9.0 | 10.0 | 11.0 | 12.0 | 13.0 | 14.0 | 15.0 | 16.0 | 17.0 | 18.0 | 19.0 | 20.0
 | 0 | 0.22222 | 0.38095 | 0.5 | 0.59259 | 0.66667 | 0.72727 | 0.77778 | 0.82051 | 0.85714 | 0.88889 | 0.91667 | 0.94118 | 0.96296 | 0.98246 | 1
R0
R
r
r+r
O2
CO2
CA: oxygen concentration
CAb = CA0
(core)
R
R0
Oxygen concentration Profile at time t
Finally determine the flux of oxygen to the surface of the core:
(center)

## Slide 28: Mass Balance on Carbon (C)
In – out + gen = accumulation
R0
R
r
r+r
O2
CO2
Elemental C does not enter or leave the surface
r’’C: rate of C gen. per unit surface area of core (mol/s·m2)
rC: density of solid C fC: fraction of the volume of the core that is C
Change in the mass of the carbon core
Simplify mass balance:
The rate of carbon disappearance (-dR/dt) is equal to the rate of oxygen flux to the surface of the core, -WO2 = WCO2, and this occurs at a radius of R so:

## Slide 29: Time Required to Shrink Core to Radius R
Substitute r’’c into -dR/dt, get like terms together, integrate, & solve for t
Integrate over 0 to t & R0 to R
Get common denominators
R0
R
r
r+r
O2
CO2

## Slide 30: Time Required to Shrink Core to Radius R
Solve for t:
R0
R
r
r+r
O2
CO2
Factor out R02/6
Factor out -1
At the core of the catalyst particle, R=0, then:
Complete regeneration

## Slide 31: L20: Internal Diffusion Effects in Spherical Catalyst Particles
Internal diffusion: diffusion of the reactants or products from the external pellet surface (pore mouth) to the interior of the pellet. (Chapter 12)
When the reactants diffuse into the pores within the catalyst pellet, the concentration at the pore mouth will be higher than that inside the pore and the entire catalytic surface is not accessible to the same concentration.
Porous catalyst particle
CAb
External diffusion
CAs
External surface
Internal diffusion
CA(r)
Though A is diffusing inwards, convention of shell balance is flux is in direction of increasing r. (flux is positive in direction of increasing r). In actuality, flux of A will have a negative sign since it moves inwards.

## Slide 32: Basic Molar Balance for Differential Element
An irreversible rxn A→B occurs on the surface of pore walls within a spherical pellet of radius R:
r
R
CAs
Rate of A in at r = WAr · area =
Rate of A out at r - r = WAr · area =
The mole balance over the shell thickness r is:
r’A: rate of reaction per mass of catalyst (mol/g•s)
c: mass of catalyst per unit volume of catalyst (catalyst density)
rm: mean radius between r and r - r
r+Dr
Spherical shell of inner radius r & outer radius r+Dr
IN - OUT + GEN =ACCUM
Volume of shell
Divide by -4pDr & take limit as Dr →0
Differential BMB in spherical catalyst particle

## Slide 33: Diffusion Equation (Step 2)
r
R
CAs
r+Dr
IN - OUT + GEN =ACCUM
Steady state assumption implies equimolar counter diffusion, WB = -WA (otherwise A or B would accumulate)
bulk diffusivify
tortuosity (distance molecule travels between 2 pts/actual distance between those 2 pts) (typical ~ 3.0)
pellet porosity (Vvoid space/Vvoid & solid) (typical ~ 0.4)
constriction factor (typical ~ 0.8)
Must use effective diffusivity, De, instead of DAB to account for:
Tortuosity of paths
Void spaces
Pores having varying cross-sectional areas

## Slide 34: Diffusion & Rxn in a Spherical Catalyst
r
R
CAs
Write the rate law based on surface area:
Relate r’A to r’’A by:
Insert the diffusion eq & the rate eq into the BMB:
Boundary Conditions:
CA finite at r=0 CA = CAs at r =R
Solve to get CA(r) and use the diffusion equation to get WAr(r)

## Slide 35: Dimensionless Variables
Put into dimensionless form
Boundary Conditions:
Y =1 at l=1 Y =finite at l=0
Thiele modulus for rxn of nth order ≡ fn
Subscript n = reaction order
fn is small: surface reaction is rate limiting
fn is large: internal diffusion is rate limiting
The solution for a 1st order rxn:
R
r=0
small 1
medium 1
large 1
small 1: surface rxn control, significant amount of reactant diffuses into pellet interior w/out reacting
large 1: surface rxn is rapid, reactant is consumed very closed to the external surface of pellet (A waste of precious metal inside of pellet)

## Slide 36: Internal Effectiveness Factor, h
For example, when n=1 (1st order kinetics, -r’’As )
Internal effectiveness factor:
(1) the relative importance of diffusion and reaction limitations
(2) a measurement of how far the reactant diffuses into the pellet before reacting

## Slide 37: Internal Diffusion & Overall Rxn Rate
h quantifies how internal diffusion affects the overall rxn rate
As particle diameter ↓, fn ↓, h→1, rxn is surface rxn limited
As particle diameter ↑, fn ↑, h→0, rxn is diffusion limited
f1
h
1
0.2
2
10
4
6
8
1
0.8
0.6
0.4
0.1
0.2
Internal diffusion limited
Reaction limited
Effectiveness factor vs fn
This analysis was for spherical particles. A similar approach can be used to evaluate other geometries, non-isothermal rxn, & more complex rxn kinetics

## Slide 38: Effectiveness Factor & Rxn Rate
surface-reaction-limited
f1 is large, diffusion-limited reaction inside the pellet (external diffusion will have a negligible effect on the overall rxn rate because internal diffusion limits the rxn rate)
Overall rate for 1st-order rxn
internal-diffusion-limited:

## Slide 39: Clicker Question
Overall rate for 1st-order rxn
When the overall rate of rxn when the reaction is limited by internal diffusion, which of the following would decrease the internal diffusion limitation?
decreasing the radius R of the particle
increasing the concentration of the reactant
increasing the temperature
(d) increasing the internal surface area
(e) Both a and b

## Slide 40: Total Rate of Consumption of A in Pellet, MA (mol/s)
At steady state, net flow of A into pellet at the external surface completely reacts within the pellet
Overall molar rxn rate = total molar flow of A into catalyst pellet
MA = (external surface area of pellet) x (molar flux of A into pellet at external surface)
MA =the net rate of reaction on and within the catalyst pellet