## Slide 1: Review: Steps in a Heterogeneous Catalytic Reaction
1. Mass transfer of A to surface
2. Diffusion of A from pore mouth to internal catalytic surface
3. Adsorption of A onto catalytic surface
4. Reaction on surface
5. Desorption of product B from surface
6. Diffusion of B from pellet interior to pore mouth
7. Diffusion of B from external surface to the bulk fluid (external diffusion)
Ch 10 assumes steps 1,2,6 & 7 are fast, so only steps 3, 4, and 5 need to be considered

## Slide 2: Review: Adsorption Step
Assume the total # of active sites remains constant (no catalyst deactivation occurs):
A(g) + S ⇌ A·S
S: open (vacant) surface site A·S: A bound to a surface site
The adsorption of A (gas phase) on an active site S is represented by:
A
I
-S-S-S-
Rate of adsorption = rate of attachment – rate of detachment
partial pressure of A
Molar conc of vacant sites on surface
A
-S-S-S-
Using adsorption equilibrium constant (KA)
Equation I
Surface
Vacant active site
A
B
Cv is not measurable, but the total # of sites, Ct can be measured
Review: Site Balance
Ct = Cv + CA·S + CB·S
Site balance:
Use to express Cv in terms of measurable species

## Slide 3: Review: Surface Reaction Step
After the molecule is adsorbed onto the surface, it can react by a few different mechanisms
1. Singe site mechanism: Only the site to which the reactant is absorbed is involved in the reaction
A
I
-S-
⇌
B
I
-S-
A·S ⇌ B·S
2. Dual site mechanism: Adsorbed reactant interacts with another vacant site to form the product
A
I
-S-S-S
⇌
B
I
-S-S-S-
A·S + S ⇌ S + B·S
Equation IIa
Equation IIb
3. Eley-Rideal mechanism: reaction between adsorbed reactant and a molecule in the gas phase
⇌
C
I
-S-S-S-
A·S + B(g) ⇌ C·S
Equation IIc
A
I
-S-S-S
B

## Slide 4: Review: Desorption Step
Products are desorbed into the gas phase
C
I
-S-S-S-
⇌
C
-S-S-S-
C·S ⇌ C + S
Equation III
Note that the desorption of C is the reverse of the adsorption of C
Also the desorption equilibrium constant KD,C is the reciprocal of the adsorption equilibrium constant KC
Substituting 1/KC for KD,C in the rate equation for product desorption gives:

## Slide 5: Review: Evaluating a Catalytic Reaction Mechanism
Collect experimental data from test reactor
Derive a rate law
  Select among types of adsorption, surface reaction, and desorption
  Write rate laws for each individual step, assuming all are reversible
  Postulate which step is rate limiting
    Surface reaction step is rate limiting ~70% of the time!
    Use non-rate-limiting steps to eliminate the surface concentration terms that cannot be measured
      Assume PSSH (rate of ads = rate of surface rxn = rate of desorp)
        No accumulation of species on the surface or near interface
        Each species adsorbed on surface is a reactive intermediate
      Net rate of formation of species i adsorbed on the surface is 0, ri·S=0
See if rate law is consistent with data
If not, then try other surface mechanism (i.e., dual-site adsorption or Eley-Rideal) or choose a different rate-limiting step (adsorption or desorption)

## Slide 6: L18: CVD & Catalyst Deactivation
Chemical vapor deposition (CVD)
  Important process in the formation of microcircuits (electrically interconnected films ICs), microprocessors & solar cells
  Used to deposit thin films of material, such as Si, SiO2, & germanium (Ge)
  Mechanism of CVD is similar to those of heterogeneous catalysis except that site concentration (CV) is replaced w/ fraction of surface coverage (fV)
Si
Si
Si
Si
Si
H
H
silicon hydride
adsorption
Si
Si
Si
Si
Si
H
H
Si
Si
Si
Si
Si
Surface reaction
H2
No desorption occurs, the product, Si, remains attached to the surface, forms a new surface

## Slide 7: Growth of Silicon Film by CVD
Write out elementary reactions and assume a rate-limiting step
1. Adsorption
Rate of adsorption = rate of attachment – rate of detachment
2. Surface reaction:
Si
Si
Si
Si
Si
H
H
Si
Si
Si
Si
Si
H
H
Si
Si
Si
Si
Si
adsorption
Surface
reaction
fv & fSiH2: fraction of the surface covered by vacant sites or SiH2, respectively
Surface coverage is in terms of fraction of surface, not conc of active sites

## Slide 8: Growth of Germanium Films by CVD
What is the rate of Ge deposition if the surface reaction is rate limiting?
r”Dep=kdisPGeCl4-k-disPGeCl2PCl2
r"Dep=kAPGeCl2fv -k-AfGeCl2
r”Dep=kHPH2fv2 -k-HfH2
r”Dep=kSfGeCl2fH2 -k-S CGePHCl2fv2
r”Dep=kSfGeCl2fH2
Gas-phase dissociation
Adsorption (1)
Adsorption (2)
Surface reaction
Surface reaction is believed to be the rate-limiting step
Germanium films have applications in microelectronics & solar cell fabrication

## Slide 9: Growth of Germanium Films by CVD
Gas-phase dissociation
Adsorption (1)
Adsorption (2)
Surface reaction
Surface reaction is believed to be the rate-limiting step:
ks: surface specific reaction rate (nm/s)
fH2: fraction on the surface occupied by H2
fGeCl2: fraction of the surface covered by GeCl2
Germanium films have applications in microelectronics & solar cell fabrication
Rate of Ge deposition (nm/s):
*Surface coverage is in terms of fraction of surface, not conc of active sites

## Slide 10: Catalyst Deactivation
Thus far, we assumed the total conc. of active sites on the surface was constant, which means the catalyst’s activity is constant throughout its lifetime
In reality, there is a gradual loss of catalytic activity (active sites on surface of the catalyst) as the reaction takes place
Main types of catalyst deactivation
  Sintering (aging): loss of active surface due to high temperature
    Coking or fouling: carbonaceous material (coke) deposits on surface
    Poisoning: molecules irreversibly bind to the active site
We will evaluate the kinetics of general catalyst deactivation and these specific types

## Slide 11: Catalyst Deactivation Kinetics
Adjustments for catalyst decay need to be made in the design of reactors
Catalyst activity a(t) is used as a quantitative specification
Catalyst activity at time t:
Reaction rate for catalyst used for time t
Reaction rate for fresh, unused catalyst
For fresh, unused catalyst,
Rate of consumption of reactant A on catalyst used for time t is:
a(t): time-dependent catalyst activity k(T): T-dependent specific rate constant
fn(CA, CB…etc): function of gas-phase conc. of reactants, products & contaminants
Rate of catalyst decay:
Function of activity
Temperature-dependent specific decay constant
Functionality of rd on reacting species conc. h=1: no conc dependence; h=Cj: linearly dependent on concentration

## Slide 12: Sintering (Aging)
Loss of active surface area resulting from the prolonged exposure to high gas-phase temperatures
Active surface area is lost by
  Crystal agglomeration and growth of metals deposited on support
  Narrowing or closing of pores inside the catalyst pellet
  Surface recrystallization
  Elimination of surface defects (active sites)
Sintering is usually negligible at temperatures below 40% of the melting temperature of the solid
Second-order decay of reaction rate with respect to present activity:
Catalyst activity at time t:
Sintering decay constant:

## Slide 13: Coking (Fouling)
Common to reactions involving hydrocarbons
A carbonaceous (coke) material is deposited on surface of catalyst
Concentration of carbon on surface (g/m2):
Coking can be reduced by running at high pressure & hydrogen-rich feeds
Catalyst deactivated by coking is often regenerated by burning off the carbon
Catalyst activity at time t:
A & n are fouling parameters
(one of many different expressions for a(t))
m is a fouling parameter

## Slide 14: Poisoning
Poisoning molecule is irreversibly chemisorbed to active sites
Reduces number of active sites available for reaction
Catalyst can be poisoned by reactants, products, and impurities
For the overall reaction:
a(t): time-dependent catalyst activity
kd: specific decay constant
CP: concentration of the poison

## Slide 15: Moving-Bed Reactor
Reactant & catalyst enter at top of reactor
Reactant & catalyst flow down the length of the reactor together as a plug
Product and spent catalyst (black) flow out of reactor outlet
Spent catalyst is regenerated by passing it through a separate regeneration unit, and newly regenerated catalyst is fed back into the top of the reactor
When catalyst decay occurs at a significant rate, they require frequent regeneration or replacement of the catalyst
Moving-bed reactor enables continuous regeneration of spent catalyst
Operates in the steady state, like a PBR

## Slide 16: Moving-Bed Reactor Design
Reactants
u0 (dm3/s)
fresh catalyst US (g/s)
Z
Z + DZ
W
W + DW
Products & coked catalyst
Catalyst flow US << reactant flow u0
As far as the reactants are concerned, reactor acts like a PBR:
Decay rate must be in terms of W (da/dW) not t (da/dt)
US relates W to t→ use US to convert da/dt to da/dW
Relate t to US:
Multiply dt/dW by -da/dt to get –da/dW:
If the rate of consumption of A for catalyst used for time t:
Catalyst activity vs position in PBR
Integrate to get a(W)

## Slide 17
A→B Given constant T, pure A in feed, and 1st order kinetics for reaction & catalyst deactivation, find XA(t) in a fluidized batch reactor of constant volume
Rate of deactivation:
Rate of rxn:
Solve the batch reactor design eq for XA. The batch reactor design eq must be combined with the rate eq. The rate eq contains ‘a’, so we need to use the rate of deactivation to find how ‘a’ varies w/ time. We will determine how ‘a’ varies with time by integrating the rate of deactivation eq & solving for ‘a’:
Insert a into the rate eq:
Batch reactor design eq:
Integrate & solve for XA